## Slide 1
Response of Majorana Electric Multipoles to Strain
in Topological Crystalline Superconductors
Yuki Yamazaki1, Shingo Kobayashi2, Ai Yamakage1
Nagoya Univ1., RIKEN (CEMS)2

## Slide 2
Topological Superconductor (TSC)
Bulk
MFs
E
k
The surface states behave as a Majorana fermions (MFs)
One-dimensional
(1D) TSC
3D TSC
MFs on a edge of the system
MFs on a surface
of the system
A fully or partially (bulk) gapped superconductor with a gapless state on the surface of the system
Semiconductor nanowire of InSb
Zero bias peak
due to MFs
Tunneling conductance
Conductance by PCS
in Ag paste part

## Slide 3
・ MFs form a Kramers pair (Majorana Kramers pair (MKP))
Do MKP necessarily vanish due to breaking of TRS? (applied magnetic field)
MKPs are protected by crystalline symmetry
K. Shiozaki and M. Sato, Phys. Rev. B 90, 165114 (2014).
M. Sato and S. Fujimoto, Phys. Rev. B 79, 094504 (2009).
SB. Chung and S.C. Zhang, Phys. Rev. Lett. 103, 235301 (2009).
・ a single MKP is stable for perturbations that do not break the TRS
E
k
Magnetic field B
？
Bulk
MFs
E
k
Topological superconductor with time-reversal symmetry (TRS)
MKPs remain gapless when a magnetic field is applied in a
specific direction (MKPs exhibit anisotropic magnetic response)

## Slide 4
TRS + Crystalline symmetry（Topological crystalline superconductor）
Anisotropic Magnetic Response＝Majorana Magnetic Multipole
Crystalline symmetry preserving the surface
There is a direction of the magnetic field
where chiral symmetry is not broken!
Zeeman term
Chiral symmetry
Magnetic winding number
TCSC
Bulk
MFs
B
Y. Xiong, A. Yamakage, S. Kobayashi, M. Sato, and Y. Tanaka, Crystals 7, 58 (2017).
S. Kobayashi, A. Yamakage, Y. Tanaka, and M. Sato, Phys. Rev. Lett. 123, 097002 (2019).

## Slide 5
Crystalline
symmetry
Detection of MFs
Bｚ
What can we know from the external
field response of MFs?
Identification of
superconducting symmetry
superconducting
symmetry
TCSC

## Slide 6
Majorana Electric Multipole (MEM)
TRS
Majorana
Operator
Coupled only with
magnetic field
TRS + Crystalline symmetry
In some cases, double MKPs are stable
Only a single MKP（ ） is stable （ ）
Y. Yamazaki, S. Kobayashi, and A. Yamakage,
J. Phys. Soc. Jpn. 89, 043703 (2020).
S. Kobayashi, Y. Yamazaki, A. Yamakage,
and M. Sato, Phys. Rev. B 103, 224504 (2021).
Electrical
external field
Owing to the crystalline symmetry, there are electric multipoles with various symmetries
Bulk
MFs
Magnetic field

## Slide 7
superconducting
symmetry
Purpose of our study
To reveal the symmetry of the Majorana electric multipole
for all wall paper groups (WGs) and pair potentials
Result
Crystalline symmetry
Detection of MFs
Identification of
superconducting symmetry
Y. Yamazaki, S. Kobayashi, and A. Yamakage,
J. Phys. Soc. Jpn. 90, 073701 (2021).

## Slide 8
where denotes irreducible representations of , and i corresponds to the degrees of freedom of the MEM; i=1,2 for two pairs of MKPs.
Coupling between Majorana Electric Multipoles (MEM) and Strain
Unsymmetrized strain tensor：
Lattice displacement field：
Transformation property by the symmetry operator g：
We consider the strain tensor as a perturbation coupled to the MEM
When the electric multipole and belong to the same irreducible representation,
they are coupled, and the coupling can be described as
Electrical
external field

## Slide 9
In this study, we consider as an effective model an antiperovskite that is a candidate material for TCSC, and where double MKPs can appear on the (001) surface
M. Oudah, A. Ikeda, J. N. Hausmann, S. Yonezawa,
T. Fukumoto, S. Kobayashi, M. Sato, and Y. Maeno:
Nat. Commun. 7, 13617 (2016).
（point group Oh）
Effective model
The matrices reflect multi-orbital properties：
Inversion symmetry：
The (001) surface respects the p4m symmetry
If the strain of or is applied, it couples to the MEM, and an energy gap opens
T. Kawakami, T. Okamura, S. Kobayashi,
and M. Sato: Phys. Rev. X 8, 041026 (2018).
Coupling between Majorana Electric Multipoles (MEM) and Strain

## Slide 10
Perturbation Hamiltonian
A1 irrep
B1 irrep
In this situation, we consider the following perturbation

## Slide 11
We have revealed the relation between the symmetry of Majorana Electric multipole and irreducible representation of the superconducting pair potential for all wall paper groups
We consider the lattice strain as an electrical perturbation and
numerically clarify the coupling with the Majorana electric multipole
Summery
Future works
Return to the bulk theory, and derive the microscopic mechanism of the coupling between the strain and MKPs
Consider dynamical strains such as induced surface acoustic waves, and calculate the spin currents and heat currents generated by dynamical strains